## Slide 1
Synthesis of Flame Retardant Composite Material Based on Waste Natural Products and Their Application as Shielding Materials Against Electromagnetic Radiation
Dr.Widad Salih Hanoosh

## Slide 2
ماذا يحتوي نبات ورق السدر
فلافونايد
مركبات فينولية
قلويات
البكتينات
بعض المواد الصابونية
حامض التانيك

## Slide 3
دراسة تأثير المستخلص المائي والكحولي لأوراق نبات السدر Zizyphusspin-csiti
على نمو بعض الانواع البكتيرية .
سلوى حمزة حسين بثينة عبد الحسن ناصر سندس وفي غني
كلية التربية للبنات-جامعة الكوفة

## Slide 4
معالجة مشاكل البشرة بورق السدر المطحون
ورق السدر المطحون وتقوية الجهاز المناعي
مد الجسم بالطاقة
ورق السدر المطحون كمهدئ للقولون
ورق السدر المطحون كمسكن لآلام المفاصل

## Slide 5
Experimental and Discussion

## Slide 6
FTIR of the Sidr Powder

## Slide 7
PAN
Reaction Schem

## Slide 8
FTIR of the Sidr Powder Polyurethane after 24 hr @ RT

## Slide 9
FTIR of the Sidr Powder Polyurethane after complete cure

## Slide 10
Mold curing

## Slide 11
Compression Molding

## Slide 13
Flammability test ( ASTM D1230-22)
Sample
2 cm

## Slide 14
Ablative Test( ASTM E285-08 2020 )

## Slide 16
Application
AS shielding material For electromagnetic radiation

## Slide 17
X-RAY RADIATION
Sample

## Slide 18
Iavr. (cpm) | I3(cpm) | I2(cpm) | I1(cpm) | Sample Thickness | Sample SM1
 | 28993 | 29175 | 28750 | 1 cm | SM1.1
 | 27750 | 27800 | 27697 | 1 cm | SM1.2
 | 31032 | 32125 | 31798 | 1 cm | SM1.3
 | 8088 | 8094 | 8172 | 2 cm | SM1.1+SM1.2
 | 8567 | 8573 | 8571 | 2 cm | SM1.1+SM1.3
 | 9011 | 8981 | 8990 | 2 cm | SM1.2+SM1.3
 | 2633 | 2618 | 2652 | 3 cm | SM1.1+SM1.2+SM1.3
Data obtained from X-ray detection
Note : Io = 109586 CPM

## Slide 19
Gama -RAY RADIATION
Gamma source in side
Samples holder
samples

## Slide 20
CPM and Exposure dose of gamma rate as a function of sample (SM1) thickness
Cs-127 Gamma source

## Slide 21
Polymeric composites sample
Neutron SOURCE
Am-Be Source

## Slide 22
Dose change of neutron source (Am-Be) as a function of SM1 sample thickness (cm ).

## Slide 23
The change of energy neutron source ( Am-Be) as a function of sample thickness

## Slide 24
Thank you for your Attention