## Slide 1
Sutures and needles
Surgical suture materials

## Slide 2
Sutures
Suture plays an important role in wound repair by providing hemostasis and support for healing tissue.
Tissues have different requirements for suture support, depending on the type of tissue and anticipated duration of healing. Some tissues need support for only a few days (e.g., muscle, subcutaneous tissue, skin), whereas others require weeks (fascia) or months (tendon) to heal.

## Slide 3
an ideal suture is one that will lose its tensile strength at a rate similar to that with which the tissue gains strength, and it will be absorbed by the tissue so that no foreign material remains in the wound.

## Slide 4
The ideal suture is
Easy to handle,
Reacts minimally in tissue,
Inhibits bacterial growth,
Holds securely when knotted,
Resists shrinking in tissue,
Absorbs with minimal reaction after the tissue has healed,
Is noncapillary, nonallergenic, noncarcinogenic, and nonferromagnetic
but such a material does not exist. Therefore, surgeons must choose a suture that most closely approximates the ideal for a given procedure and tissue to be sutured. A wide variety of suture and needle combinations are available.

## Slide 5
Suture size.
The smallest diameter suture that will adequately secure wounded tissue should be used in order to :
1. minimize trauma as the suture is passed through the tissue and
2. to reduce the amount of foreign material left in the wound.
There is no advantage to using a suture that is stronger than the tissue to be sutured
The most commonly used standard for suture size is the United States Pharmacopeia (USP), which denotes dimensions from fine to coarse (with diameters in inches) according to a numeric scale, with 12-0 being the smallest and 7 the largest.
The smaller the suture size, the less tensile strength it has.

## Slide 6
Flexibility.
It is determined by its torsional stiffness and diameter which influence its handling and use.
Flexible sutures are indicated for ligating vessels or performing continuous suture patterns. Less flexible sutures (e.g., wire) cannot be used to ligate small bleeders.
Nylon and surgical gut are relatively stiff compared with silk suture; braided polyester sutures have intermediate stiffness.

## Slide 7
Notes: Fffffffff

## Slide 11
Surface characteristics and coating.
The surface characteristics of a suture influence the ease with which it is pulled through tissue (i.e., the amount of friction or “drag”) and the amount of trauma caused. Rough sutures cause more injury than smooth sutures.
Smooth surfaces are particularly important in delicate tissues, such as the eye.
However, sutures with smooth surfaces also require greater tension to ensure good apposition of tissues and have less knot security
Braided materials have more drag than monofilament sutures. Braided materials often are coated to reduce capillarity, but this also provides a smooth surface. Teflon, silicone, wax, paraffin wax, and calcium stearate are used for coating sutures

## Slide 13
Capillarity.
Capillarity is the process by which fluid and bacteria are carried into the interstices of multifilament fibers.
Because neutrophils and macrophages are too large to enter the interstices of the fiber, infection may persist, particularly in nonabsorbable sutures.
All braided materials (e.g., polyglycolic acid, silk) have degrees of capillarity, whereas monofilament sutures are considered noncapillary.
Coating reduces the capillarity of some sutures, but regardless, capillary suture materials should not be used in contaminated or infected sites.

## Slide 15
Knot tensile strength.
Knot tensile strength is measured by the force in pounds that the suture strand can withstand before it breaks when knotted.
Sutures should be as strong as the normal tissue; however, the tensile strength of the suture should not greatly exceed the tensile strength of the tissue.
يجب أن تكون الغرز قوية مثل الأنسجة الطبيعية ؛ ومع ذلك ، يجب ألا تتجاوز قوة شد الخيط بشكل كبير قوة الشد للنسيج

## Slide 17
Relative knot security.
Relative knot security is the holding capacity of a suture expressed as a percentage of its tensile strength.
The knot-holding capacity of a suture material is the strength required to untie or break a defined knot by loading the part of the suture that forms the loop, whereas the suture material’s tensile strength is the strength required to break an untied fiber with a force applied in the direction of its length

## Slide 19
Specific Suturing Materials
Suture materials may be classified according to
their behavior in tissue (absorbable or nonabsorbable),
their structure (monofilament or multifilament), or
their origin (synthetic, organic, or metallic)

## Slide 21
Two major mechanisms of absorption result in the degradation of absorbable sutures.
Sutures of organic origin, such as surgical gut, are gradually digested by tissue enzymes and phagocytized,
sutures manufactured from synthetic polymers are principally broken down by hydrolysis.
Nonabsorbable sutures are ultimately encapsulated or walled off by fibrous tissue.

## Slide 22
Monofilament sutures are made of a single strand of material and therefore have less tissue drag than multifilament sutures and do not have interstices that may harbor bacteria or fluid.
Care should be used in handling monofilament suture because damaging the material with forceps or needle holders may weaken the suture and predispose it to breakage.
Multifilament sutures consist of several strands of suture that are twisted or braided together. Multifilament sutures generally are more pliable and flexible than monofilament sutures. They may be coated to reduce tissue drag and enhance handling characteristics.

## Slide 24
Absorbable Suture Materials
Absorbable suture materials (e.g., surgical gut, polyglycolic acid [Dexon, Covidien, Mansfield, Mass.], polyglactin 910 [Vicryl, Ethicon, Somerville, N.J.], polydioxanone [PDS II, Ethicon, Somerville, N.J.], polyglyconate [Maxon, Covidien, Mansfield Mass.], poliglecaprone 25 [Monocryl, Ethicon, Somerville, N.J.], glycomer 631 [Biosyn, Covidien, Mansfield, Mass.])
lose most of their tensile strength within 60 days and eventually disappear from the tissue implantation site because they have been phagocytized or hydrolyzed.
The time to loss of strength and for complete absorption varies among suture materials.

## Slide 25
Organic absorbable materials.
Catgut (surgical gut) is the most common nonsynthetic absorbable suture material.
Although once very popular, its use has decreased substantially in veterinary medicine with the appearance of strong monofilament synthetic absorbable suture materials.
The word catgut is derived from the term kitgut or kitstring (the string used on a kit, or fiddle).
Misinterpretation of the word kit as referring to a young cat led to the use of the term catgut.

## Slide 26: Catgut (surgical gut)
Surgical gut is in fact made from the submucosa of sheep intestine or the serosa of bovine intestine and is approximately 90% collagen.
It is broken down by phagocytosis and, in contrast with other suture materials, results a notable inflammatory reaction.
Surgical gut is available as plain, medium chromic, or chromic; increased tanningالدباغة generally implies prolonged strength and reduced tissue reaction.
Surgical gut is rapidly removed from infected sites or areas where it is exposed to digestive enzymes and is quickly degraded in catabolic patients. The knots may loosen when wet.

## Slide 28
Synthetic absorbable materials.
Synthetic absorbable materials generally are broken down by hydrolysis and cause minimal tissue reaction.
The time to loss of strength and to absorption is fairly constant even in different tissue.
Infection or exposure to digestive enzymes does not significantly influence the rate of absorption of most synthetic absorbable sutures.
Polyglactin 910 and polyglycolic acid are more rapidly hydrolyzed in alkaline environments, but they are relatively stable in contaminated wounds.
However, any suture that is degraded via hydrolysis may be at risk for accelerated degradation when the bladder is infected with Proteus spp.

## Slide 29
Monofilament absorbable materials.
Polydioxanone and polyglyconate are classic monofilament sutures that keep their tensile strength longer than multifilament sutures with complete absorption occurring in 6 months.
Poliglecaprone 25 and glycomer 631 are relatively new monofilament rapidly absorbable synthetic materials that are pliable, lack stiffness, and have good handling characteristics.
These sutures have good initial tensile strength that deteriorates in 2 to 3 weeks following implantation and are completely absorbed by 120 days.

## Slide 30
Multifilament absorbable materials.
Polyglycolic acid is braided from filaments extracted from glycolic acid and is available in both coated and uncoated forms.
Polyglactin 910 is a multifilament suture made of a copolymer of lactide and glycolide with polyglactin 370. It is coated with calcium stearate and its rate of loss of tensile strength is similar to that of polyglycolic acid.
Polysorb is a new synthetic absorbable suture material composed of a glycolide/lactide co-polymer. Polysorb has good initial tensile strength and is completely absorbed by 60 days.
Vicryl Rapide is a relatively new, rapidly absorbed, synthetic braided suture that has an initial strength that is comparable to nylon and gut. However, the tensile strength declines to 50% in 5 to 6 days, and it is completely absorbed in 42 days. This suture is indicated for superficial closure of mucosa, gingival closure, and periocular skin closure.
Vicryl Plus is a new suture that was designed to reduce bacterial colonization on the suture. It has been coated with an antibacterial agent, triclosan.

## Slide 31
Nonabsorbable Suture Materials
Organic nonabsorbable materials.
Silk is the most common organic nonabsorbable suture material used. It is a braided multifilament suture made by a special type of silkworm and is marketed as uncoated or coated. Silk has excellent handling characteristics and often is used in cardiovascular procedures;
It should also be avoided in contaminated sites

## Slide 32
Synthetic nonabsorbable materials.
Synthetic nonabsorbable suture materials are marketed as
1. braided multifilament threads (e.g., polyester or coated caprolactam) or
2. monofilament threads (e.g., polypropylene, olyamide, or polybutester).
These sutures are typically strong and induce minimal tissue reaction.
Nonabsorbable suture materials with an inner core and an outer sheath should not be buried in tissue because they may predispose to infection and fistulation.
The outer sheath frequently is broken, which allows bacteria to reside underneath it.

## Slide 33
Metallic sutures.
Stainless steel is the metallic suture most commonly used and is available as a monofilament or multifilament twisted wire.
Surgical steel is strong with minimal tissue reaction, but knot ends evoke an inflammatory reaction. Stainless steel has a tendency to cut tissue.
It is stable in contaminated wounds and is the standard for judging knot security and tissue reaction to suture materials.